| Começo | Mold No. | Left1 | Left2 | Right3 | Right4 | 15 min. depois | Mold No. | Left1 | Left2 | Right3 | Right4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Peso do produto | 17.7g | 17.9g | 17.3g | 17.1g |  | Peso do produto | 17.8g | 18.0g | 17.4g | 17.1g |
| Espessura EVOH | Espessura frontal | 0.05mm | 0.04mm | 0.04mm | 0.05mm | Espessura EVOH | Espessura frontal | 0.03mm | 0.04mm | 0.04mm | 0.05mm |
|  | Espessura traseira | 0.03mm | 0.03mm | 0.03mm | 0.03mm |  | Espessura traseira | 0.02mm | 0.03mm | 0.03mm | 0.05mm |
|  | Espessura da esquerda | 0.04mm | 0.03mm | 0.04mm | 0.03mm |  | Espessura da esquerda | 0.03mm | 0.03mm | 0.04mm | 0.03mm |
|  | Espessura da direita | 0.03mm | 0.03mm | 0.03mm | 0.03mm |  | Espessura da direita | 0.02mm | 0.02mm | 0.02mm | 0.03mm |
| 30 min. depois | Molde No. | Esquerda 1 | Esquerda 2 | Direita 3 | Direita 4 | 45 min. depois | Molde No. | Esquerda 1 | Esquerda 2 | Direita3 | Direita 4 |
|  | Peso do produto | 17.7g | 17.9g | 17.4g | 17.1g |  | Peso do produto | 17.6g | 18.1g | 17.3g | 17.3g |
| Espessura EVOH | Espessura Frontal | 0.03mm | 0.04mm | 0.04mm | 0.05mm | Espessura do EVOH | Espessura frontal | 0.04mm | 0.04mm | 0.05mm | 0.05mm |
|  | Espessura traseira | 0.03mm | 0.03mm | 0.04mm | 0.05mm |  | Espessura traseira | 0.02mm | 0.03mm | 0.04mm | 0.05mm |
|  | Espessura da esquerda | 0.03mm | 0.03mm | 0.03mm | 0.03mm |  | Espessura da esquerda | 0.03mm | 0.03mm | 0.03mm | 0.03mm |
|  | Espessura da direita | 0.02mm | 0.03mm | 0.03mm | 0.03mm |  | Espessura da direita | 0.02mm | 0.03mm | 0.03mm | 0.03mm |
| 60 min. depois | Molde No. | Esquerda 1 | Esquerda 2 | Direita 3 | Direita 4 | 90 min. depois | Molde No. | Direita 1 | Esquerda2 | Direita3 | Direita4 |
|  | Peso do produto | 17.6g | 17.9g | 17.4g | 17.2g |  | Peso do produto | 17.7g | 17.9g | 17.3g | 17.1g |
| Espessura EVOH | Espessura frontal | 0.05mm | 0.04mm | 0.04mm | 0.05mm | Espessura EVOH | Espessura frontal | 0.03mm | 0.05mm | 0.04mm | 0.04mm |
|  | Espessura traseira | 0.03mm | 0.03mm | 0.03mm | 0.03mm |  | Espessura traseira | 0.03mm | 0.05mm | 0.03mm | 0.05mm |
|  | Espessura da esquerda | 0.03mm | 0.03mm | 0.04mm | 0.04mm |  | Espessura da esquerda | 0.04mm | 0.03mm | 0.03mm | 0.04mm |
|  | Espessura da direita | 0.03mm | 0.02mm | 0.03mm | 0.03mm |  | Espessura da direita | 0.03mm | 0.03mm | 0.02mm | 0.03mm |
| 120 min. depois | Molde No. | Esquerda 1 | Esquerda 2 | Direita 3 | Direita 4 | 150 min. depois | Molde No. | Esquerda 1 | Esquerda 2 | Direita 3 | Direita 4 |
|  | Peso do produto | 17.6g | 17.9g | 15.5g | 17.1g |  | Peso do produto | 17.8g | 18.0g | 17.4g | 17.2g |
| Espessura EVOH | Espessura frontal | 0.04mm | 0.05mm | 0.03mm | 0.05mm | Espessura EVOH | Espessura Frontal | 0.03mm | 0.04mm | 0.04mm | 0.04mm |
|  | Espessura traseira | 0.03mm | 0.04mm | 0.03mm | 0.05mm |  | Espessura traseira | 0.03mm | 0.03mm | 0.03mm | 0.03mm |
|  | Espessura da esquerda | 0.03mm | 0.03mm | 0.03mm | 0.03mm |  | Espessura da esquerda | 0.03mm | 0.04mm | 0.03mm | 0.03mm |
|  | Espessura da direita | 0.03mm | 0.03mm | 0.03mm | 0.03mm |  | Espessura da direita | 0.03mm | 0.04mm | 0.02mm | 0.02mm |

| 180 min. depois | Molde No. | Esquerda1 | Esquerda2 | Direita3 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Peso do produto | 17.6g | 17.9g | 17.3g |  |  |  |  |  |  |  |
| Espessura EVOH | Espessura frontal | 0.04mm | 0.04mm | 0.05mm |  |  |  |  |  |  |  |
|  | Espessura traseira | 0.03mm | 0.03mm | 0.03mm |  |  |  |  |  |  |  |
|  | Espessura da esquerda | 0.03mm | 0.03mm | 0.03mm |  |  |  |  |  |  |  |
|  | Espessura da direita | 0.03mm | 0.02mm | 0.03mm |  |  |  |  |  |  |  |
| Dossel: Xingguang Chen QC: Chengsong Li Data de análise: 9 de Julho de 2009 às 10:20 |

| Begin | Mold No. | Left1 | Left2 | Right3 | Right4 | 15 min. later | Mold No. | Left1 | Left2 | Right3 | Right4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Product weight | 17.7g | 17.9g | 17.9g | 17.7g |  | Product weight | 17.7g | 17.8g | 18.4g | 17.7g |
| EVOH Thickness | Frontal thickness | 0.03mm | 0.05mm | 0.05mm | 0.05mm | EVOH Thickness | Frontal thickness | 0.04mm | 0.05mm | 0.05mm | 0.03mm |
|  | Back thickness | 0.03mm | 0.03mm | 0.03mm | 0.04mm |  | Back thickness | 0.03mm | 0.04mm | 0.02mm | 0.03mm |
|  | Left thickness | 0.03mm | 0.04mm | 0.05mm | 0.03mm |  | Left thickness | 0.03mm | 0.03mm | 0.03mm | 0.03mm |
|  | Right thickness | 0.02mm | 0.03mm | 0.04mm | 0.03mm |  | Right thickness | 0.02mm | 0.02mm | 0.03mm | 0.03mm |
| 30 min. later | Mold No. | Left1 | Left2 | Right3 | Right4 | 45 min. later | Mold No. | Left1 | Left2 | Right3 | Right4 |
|  | Product weight | 17.6g | 17.8g | 17.9g | 17.7g |  | Product weight | 17.6g | 17.8g | 18.6g | 17.7g |
| EVOH Thickness | Frontal thickness | 0.03mm | 0.04mm | 0.05mm | 0.05mm | EVOH Thickness | Frontal thickness | 0.05mm | 0.05mm | 0.07mm | 0.03mm |
|  | Back thickness | 0.04mm | 0.03mm | 0.04mm | 0.03mm |  | Back thickness | 0.03mm | 0.04mm | 0.05mm | 0.03mm |
|  | Left thickness | 0.03mm | 0.04mm | 0.03mm | 0.03mm |  | Left thickness | 0.03mm | 0.03mm | 0.05mm | 0.03mm |
|  | Right thickness | 0.03mm | 0.03mm | 0.04mm | 0.03mm |  | Right thickness | 0.03mm | 0.04mm | 0.04mm | 0.03mm |
| 60 min. later | Mold No. | Left1 | Left2 | Right3 | Right4 | 90 min. later | Mold No. | Left1 | Left2 | Right3 | Right4 |
|  | Product weight | 17.8g | 17.9g | 17.9g | 17.7g |  | Product weight | 17.8g | 17.9g | 18.4g | 17.7g |
| EVOH Thickness | Frontal thickness | 0.03mm | 0.05mm | 0.05mm | 0.05mm | EVOH Thickness | Frontal thickness | 0.05mm | 0.04mm | 0.05mm | 0.04mm |
|  | Back thickness | 0.04mm | 0.04mm | 0.04mm | 0.05mm |  | Back thickness | 0.03mm | 0.03mm | 0.05mm | 0.04mm |
|  | Left thickness | 0.03mm | 0.03mm | 0.05mm | 0.03mm |  | Left thickness | 0.05mm | 0.03mm | 0.04mm | 0.03mm |
|  | Right thickness | 0.04mm | 0.04mm | 0.03mm | 0.03mm |  | Right thickness | 0.03mm | 0.03mm | 0.03mm | 0.03mm |

| 120 min. later | Mold No. | Left1 | Left2 | Right3 | Right4 | 150 min. later | Mold No. | Left1 | Left2 | Right3 | Right4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Product weight | 17.7g | 17.9g | 17.9g | 17.7g |  | Product weight | 17.6g | 18.1g | 17.9g | 17.6g |
| EVOH Thickness | Frontal thickness | 0.05mm | 0.06mm | 0.05mm | 0.03mm | EVOH Thickness | Frontal thickness | 0.05mm | 0.05mm | 0.05mm | 0.05mm |
|  | Back thickness | 0.03mm | 0.05mm | 0.04mm | 0.04mm |  | Back thickness | 0.05mm | 0.04mm | 0.04mm | 0.03mm |
|  | Left thickness | 0.03mm | 0.03mm | 0.04mm | 0.02mm |  | Left thickness | 0.03mm | 0.03mm | 0.05mm | 0.03mm |
|  | Right thickness | 0.03mm | 0.02mm | 0.03mm | 0.02mm |  | Right thickness | 0.03mm | 0.03mm | 0.03mm | 0.03mm |
| Begin | Mold No. | Left1 | Left2 | Right3 | Right4 | 15 min. later | Mold No. | Left1 | Left2 | Right3 | Right4 |
|  | Product weight | 17.7g | 18.0g | 18.6g | 17.6g |  | Product weight | 17.6g | 17.9g | 18.3g | 17.7g |
| EVOH Thickness | Frontal thickness | 0.05mm | 0.05mm | 0.05mm | 0.05mm | EVOH Thickness | Frontal thickness | 0.04mm | 0.05mm | 0.05mm | 0.05mm |
|  | Back thickness | 0.05mm | 0.03mm | 0.04mm | 0.03mm |  | Back thickness | 0.03mm | 0.04mm | 0.04mm | 0.04mm |
|  | Left thickness | 0.03mm | 0.03mm | 0.06mm | 0.04mm |  | Left thickness | 0.03mm | 0.04mm | 0.05mm | 0.04mm |
|  | Right thickness | 0.03mm | 0.02mm | 0.04mm | 0.03mm |  | Right thickness | 0.03mm | 0.03mm | 0.04mm | 0.03mm |
| Tester: Xingguang Chen QC: Chengsong Li Testing date: July 9, 2009 at 15:45 |